## Slide 1: Shape Memory Alloys: Wing Morphing Technology
Daniel Gracias Guide: Prof. Anirban Patra
25th November `22
IIT Bombay

## Slide 2: Report
Link

## Slide 3: Shape Memory Behaviour
One-Way Shape Memory Effect Retention of deformed state on removal of load followed by recovery of original shape on heating
Two-Way Shape Memory Effect ‘Memorization’ of two different shapes corresponding to two different temperatures
Superelasticity Recovery of high strains (up to 8.5%) on removal of load
Notes: Superelasticity

## Slide 4: History
Superelasticity in Au-Cd system discovered in 1932 Arne Ölander
The fundamental phenomena behind the shape memory behaviour reported in 1949-51
Discovery of Nitinol (Ni-Ti, 50 at% Ni) 1962
  Cheaper
  Safer
  Superior Thermomechanical Properties
Notes: Predominantly used for commercial applications

## Slide 5: Martensitic Phase Transformation
On cooling Austenite, Martensite formation starts at Ms and is completed at Mf
On reheating, Austenite formation starts at As and is completed at Af
Hysteresis
Mf < Ms < As < Af
Typical Behaviour of SMAs under constant stress
D.E Hodgeson; Shape Memory Applications, Inc; www.sma-inc.com
Notes: Hysterisis: dependence on previous state. Fatigue

## Slide 6: Martensitic Phase Transformation
Austenite Phase: CsCl-type 𝐵2 superlattice ()
Martensite: close-packed monoclinic structure ()
Transformation is diffusion-less: induced by either temperature or stress
Lattice distortion
Invariant Planes: Leads to twinning ‘Self-accommodating’
Deformation
  Detwinning in Martensite
  Slip or stress induced phase transformation in Austenite
H Miyazaki, H.Y Kim, ‘Basic characteristics of titanium– nickel (Ti–Ni)- based and titanium–niobium (Ti–Nb)-based alloys’
S Barbarino, E I Saavedra Flores, R M Ajaj, I Dayyani, M I Friswell, ‘A review on shape memory alloys with applications to morphing aircraft’ , ‘Smart Materials and Structures’, 23 (2014)
Notes: Instantaneous change; maintains macroscopic shape

## Slide 7: Thermomechanical Behaviour
One way SME: no macroscopic shape difference between twinned martensite and austenite. Heating deformed martensite to Af results in reversion to original shape (a)
Superelasticity: In temperature range Af <T< Ts, deformation is via stress induced martensitic transformation. Since austenite is the stable phase, reversion to original shape
Schematic Stress-Strain Behaviour in Various Temperature Ranges
H Miyazaki, H.Y Kim, ‘Basic characteristics of titanium– nickel (Ti–Ni)- based and titanium–niobium (Ti–Nb)-based alloys’
Notes: Deformation behaviour is temp sensitive. 𝑇s is the temperature above which deformation occurs via slip as opposed to martensitic transformation.

## Slide 8: Training
TRIP: TRansformation Induced Plasticity Irrecoverable strain in polycrystals
Higher in the initial cycles, reduces with the number of cycles, eventually stabilizing to zero
Eliminates twinned martensite
Stabilised thermomechanical response: Two way SME
Experimental results for training via isobaric thermal cycling
D J Hartl, D C Lagoudas, ‘Aerospace applications of shape memory alloys’, ‘IMech E’ 221(2007), pp. 535-549

## Slide 9
Lagoudas DC. Shape memory alloys: modeling and engineering applications. 1st ed. New York: Springer; 2010

## Slide 10: Applications
Advantages
  High actuation density
  Complex actuation
  Thermal Response
Challenges
  Actuation Frequency
  Accuracy
  Temperature control
  Efficiency
  Fatigue

## Slide 11: Applications
Automotive
  Linear Actuators: rear view mirror, climate control flaps, etc
  Thermal Actuators: engine temperature control, etc
Robotics
  Artificial muscles
  Microactuators
Biomedical
  Dentistry
  Stents
  Implants
Aerospace
  Vibration Dampers
  Exhaust Nozzle
  Flow mixing chevrons
  Wing Morphing

## Slide 12: Wing Morphing
Optimisation based on flight regime
  Lift to drag ratio
SMA actuators for wing morphing:
Continuous, hinge-less
Lightweight
https://en.wikipedia.org/wiki/Airfoil

## Slide 13: DARPA Smart Wing (1998)
16% Scaled down model of F-18 military aircraft wing
Wind tunnel testing
SMA actuated parameters:
  Angle of attack (twist) by means of SMA torque tubes
    Provided 5° twist at wing tip
  Trailing edge by means of SMA wires
    Flap and aileron
J N Kudva et al, ‘Overview of the DARPA/AFRL/NASA Smart Wing Program’ Proceedings of SPIE Conference on Industrial and Commercial Applications of Smart Structures, 1999

## Slide 14: Strelec et al. (2003)
Optimisation tool (Genetic Algorithm): aerodynamic, structural and thermal analysis to converge design; optimise L/D
Nitinol wires for actuation of leading and trailing edge
Wind tunnel tested
Provided trailing edge deflection of 6mm
Strelec J K, Lagoudas D C, Khan M A and Yen J, ‘Design and implementation of a shape memory alloy actuated reconfigurable airfoil’ J. Intell. Mater. Syst. Struct (2003)

## Slide 15: NASA Spanwise Adaptive Wing (2018)
Folding of outboard portions
Up to 70° in both directions
Weighs 80% less than traditional systems with same functionality
Autonomous flight tested
https://www.nasa.gov/centers/armstrong/feature/nasa-tests-new-alloy-to-fold-wings-in-flight.html

## Slide 16: NASA Spanwise Adaptive Wing (2018)
https://www.nasa.gov/centers/armstrong/feature/nasa-tests-new-alloy-to-fold-wings-in-flight.html
https://www.youtube.com/watch?v=9y1kkG2_QpE&t=3s

## Slide 17: References
Jaronie Mohd Jani, Martin Leary, Aleksandar Subic, Martin A. Gibson, ‘A review of shape memory alloy research, applications and opportunities’, ‘Materials and Design’, 2013, pp. 1078-1080
H Miyazaki, H.Y Kim, ‘Basic characteristics of titanium– nickel (Ti–Ni)- based and titanium–niobium (Ti–Nb)-based alloys’ (Woodhead Publishing Limited (2011), pp. 15-29
Jose Maria Gallardo Fuentes, Paul Gumpel, Joachim Strittmatter, ‘Phase change behaviour of nitinol shape memory alloys: Influence of heat and thermomechanical treatments’, ‘Advanced Engineering Materials’, Volume 4 Issue 7 (2002), pp. 437-440
D J Hartl, D C Lagoudas, ‘Aerospace applications of shape memory alloys’, ‘IMech E’ 221(2007), pp. 535-549
A.Y.N. Sofla, S.A. Meguid, K.T. Tan, W.K. Yeo, ‘Shape morphing of aircraft wing: Status and challenges’, ‘Materials and Design’ 31(2010), pp. 1284-1292
S Barbarino, E I Saavedra Flores, R M Ajaj, I Dayyani, M I Friswell, ‘A review on shape memory alloys with applications to morphing aircraft’ , ‘Smart Materials and Structures’, 23 (2014)
J N Kudva et al, ‘Overview of the DARPA/AFRL/NASA Smart Wing Program’ Proceedings of SPIE Conference on Industrial and Commercial Applications of Smart Structures, 1999`
Strelec J K, Lagoudas D C, Khan M A and Yen J, ‘Design and implementation of a shape memory alloy actuated reconfigurable airfoil’ J. Intell. Mater. Syst. Struct (2003)
‘NASA Tests New Alloy to Fold Wings in Flight’ - Matt Kamlet (https://www.nasa.gov/centers/armstrong/feature/nasa-tests-new-alloy-to-fold-wings-in-flight.html)